UNIT I

General Principles of Metallurgy

B.Sc. (Hons.) Chemistry  |  Delhi University  |  First Year

Topics Covered (6 Hours)

1. Chief Modes of Occurrence of Metals 2. Ellingham Diagrams — Reduction using C and CO 3. Electrolytic Reduction 4. Hydrometallurgy — Cyanide Process for Ag and Au 5. Purification: Electrolytic, Van Arkel-De Boer, Zone Refining 6. Metals and Alloys in Ancient and Medieval India

# 1. Chief Modes of Occurrence of Metals

Metals occur in nature either in the free (native) state or in the combined state as ores. The mode of occurrence is determined primarily by the standard electrode potential (E°) of the metal.

## 1.1 Standard Electrode Potential and Occurrence

The standard electrode potential (E°) of Mⁿ⁺/M reflects how easily a metal is oxidised. Metals with high negative E° (electropositive metals) are easily oxidised and occur only as compounds. Metals with high positive E° are difficult to oxidise and occur in the native state.

| E° Range | Occurrence | Examples |
| --- | --- | --- |
| Very negative (< −1.5 V) | Combined state only; as oxides, chlorides, silicates | Na, K, Mg, Al, Ca |
| Moderately negative (−1.5 to ~0 V) | Combined state; mainly as sulphides, oxides, carbonates | Zn, Fe, Pb, Sn, Ni |
| Near zero to moderately positive | Mostly as sulphides; some native metal | Cu, Hg, Ag (partially) |
| Highly positive (> +0.5 V) | Native / free state | Au, Pt, Pd, Os |

Key Rule of Thumb

The more electropositive (more negative E°) a metal is, the more reactive it is, and the more likely it is to be found in a combined state. The more electronegative (positive E°) a metal is, the less reactive it is and the more likely it exists in the free state.

## 1.2 Important Ore Types

| Ore Type | Composition | Examples |
| --- | --- | --- |
| Native metals | Free elemental metal | Au, Ag, Pt, Cu (sometimes) |
| Oxides | Metal + O | Fe₂O₃ (haematite), Al₂O₃ (bauxite), MnO₂ |
| Sulphides | Metal + S | PbS (galena), ZnS (zinc blende), Cu₂S (chalcocite) |
| Carbonates | Metal + CO₃²⁻ | CaCO₃ (calcite), ZnCO₃ (smithsonite), FeCO₃ (siderite) |
| Halides | Metal + halide | NaCl (rock salt), CaF₂ (fluorspar), AlF₃·3NaF (cryolite) |
| Silicates | Metal silicate | Be₃Al₂Si₆O₁₈ (beryl), ZrSiO₄ (zircon) |
| Sulphates | Metal + SO₄²⁻ | BaSO₄ (barytes), CaSO₄·2H₂O (gypsum) |

# 2. Ellingham Diagrams

An Ellingham diagram is a plot of ΔG° (standard Gibbs free energy of formation) vs. temperature for the oxidation reactions of metals and the corresponding reduction reactions of their oxides. It was developed by Harold Ellingham (1944).

## 2.1 Basis: Thermodynamic Principle

For the reaction: M + O₂ → MO₂,  ΔG° = ΔH° − TΔS°

The plot of ΔG° vs T is approximately linear. The slope is −ΔS° of the reaction.

| Feature | Explanation |
| --- | --- |
| Lines slope upward (positive slope) | Metal oxidation: ΔS° is negative (solid + gas → solid), so −ΔS° = positive slope |
| Carbon (C→CO) line slopes downward | C + ½O₂ → CO: 1 mol gas → 1 mol gas, but C+O₂→2CO produces 2 mol gas. Large positive ΔS° → negative slope |
| CO→CO₂ line is nearly flat | Same moles of gas on both sides; ΔS° ≈ 0 |
| Kink / change in slope | Occurs at melting point, boiling point, or phase transition of the metal (ΔS changes suddenly) |

## 2.2 How to Read the Ellingham Diagram

The fundamental rule: A metal oxide can be reduced by a reducing agent if the ΔG° line of the reducing agent lies BELOW the ΔG° line of the metal oxide at that temperature.

- Reduction is feasible when: ΔG°(reducing agent oxidation) < ΔG°(metal oxide formation) → net ΔG° < 0

- The crossover point is the minimum temperature at which reduction becomes thermodynamically feasible.

## 2.3 Using Carbon (C) as Reducing Agent

Carbon can reduce metal oxides in two ways:

- C + O₂ → CO₂:  ΔG° nearly constant with T (flat line)

- 2C + O₂ → 2CO:  ΔG° becomes increasingly negative with T (strongly descending line)

Critical Observation: Carbon Wins at High Temperature

At high temperatures, the 2C+O₂→2CO line (steeply negative slope) crosses below the lines of most metal oxides. This means carbon can reduce most metal oxides at sufficiently high temperatures. This is the basis of the blast furnace for iron. Example — Reduction of Fe₂O₃: Fe₂O₃ + 3C → 2Fe + 3CO (feasible above ~700°C) Example — Reduction of ZnO: ZnO + C → Zn + CO (feasible above ~950°C) However, carbon cannot reduce the oxides of very electropositive metals like Al₂O₃, MgO, CaO at any practical temperature because their ΔG° lines lie far below carbon's lines.

## 2.4 Using Carbon Monoxide (CO) as Reducing Agent

CO reduces metal oxides via: CO + MO → M + CO₂

The reaction: CO + ½O₂ → CO₂ has a nearly flat ΔG° line. This means CO is effective as a reducing agent over a limited temperature range (roughly up to 700°C). At higher temperatures, the C→CO line goes lower, making solid C more effective than CO.

| Reducing Agent | Effective Temperature Range | Key Reduction Examples |
| --- | --- | --- |
| CO | Low to moderate (~400–700°C) | Fe₂O₃→Fe (in lower blast furnace zones); PbO→Pb; NiO→Ni |
| C (to CO₂) | Moderate (~700–900°C) | Some oxide reductions |
| C (to CO) | High (>900°C) | Fe₂O₃, ZnO, SnO₂ (most industrial smelting) |

## 2.5 Limitations of Ellingham Diagrams

- Assumes all reactants and products are in standard states (pure solids/gases at 1 atm).

- Thermodynamic predictions only — does not account for reaction kinetics.

- Does not account for the formation of mixed oxides or slag.

- Cannot predict the efficiency of separation of the metal from the slag.

# 3. Electrolytic Reduction

For metals whose oxides cannot be reduced by carbon or CO (very electropositive metals like Al, Na, Mg, Ca), electrolytic reduction is used. The metal oxide or halide is melted and electrolysed.

## 3.1 Hall-Héroult Process (Aluminium)

The most important industrial electrolytic reduction. Developed independently by Charles Hall (USA) and Paul Héroult (France) in 1886

### Raw Material

- Ore: Bauxite (Al₂O₃·2H₂O), purified to Al₂O₃ (alumina) by the Bayer process.

### Electrolyte

- Al₂O₃ dissolved in molten cryolite (Na₃AlF₆) at ~960°C (pure Al₂O₃ melts at 2050°C — too high).

- Fluorspar (CaF₂) added to lower melting point and increase conductivity.

### Electrodes

- Cathode: Carbon lining of the steel tank.

- Anode: Carbon/graphite rods (consumed during reaction).

### Reactions

- Cathode: Al³⁺ + 3e⁻ → Al  (molten Al sinks to bottom)

- Anode:   2O²⁻ → O₂ + 4e⁻  (oxygen oxidises carbon anode: C + O₂ → CO₂)

### Key Features

- Anodes must be replaced periodically due to oxidation.

- Energy-intensive process (~15 kWh per kg of Al produced).

- Molten Al is tapped off from the bottom of the cell.

Why Cryolite?

Pure Al₂O₃ has a melting point of 2050°C — far too high for practical electrolysis. Dissolving Al₂O₃ in molten cryolite (Na₃AlF₆) at ~960°C makes the process feasible. Cryolite acts as a solvent for alumina, lowering the operating temperature dramatically.

## 3.2 Down's Process (Sodium)

Used to produce sodium metal by electrolysis of molten NaCl.

| Component | Detail |
| --- | --- |
| Electrolyte | Molten NaCl + CaCl₂ (lowers m.p. from 801°C to ~600°C) |
| Cathode (iron ring) | Na⁺ + e⁻ → Na (liquid sodium floats up) |
| Anode (graphite) | 2Cl⁻ → Cl₂ + 2e⁻ |
| Separator | Iron gauze prevents Na and Cl₂ from recombining |
| Products | Sodium metal + Cl₂ gas (both commercially valuable) |

# 4. Hydrometallurgy — Cyanide Process for Silver and Gold

Hydrometallurgy refers to the extraction of metals from their ores using aqueous solutions. It operates at low temperatures and is especially useful for low-grade ores. The cyanide process (MacArthur-Forrest Process, 1887) is the most important hydrometallurgical method.

## 4.1 Cyanide Process for Silver

### Ore

Argentite (Ag₂S) or native silver in low-grade ores mixed with rock.

### Step 1 — Leaching (Dissolution in Cyanide Solution)

Crushed ore is treated with dilute NaCN or KCN solution in the presence of air (O₂):

Ag₂S + 4NaCN + ½O₂ + H₂O  →  2Na[Ag(CN)₂] + NaOH + S

Or equivalently: 4Ag + 8CN⁻ + O₂ + 2H₂O → 4[Ag(CN)₂]⁻ + 4OH⁻

The silver forms a soluble dicyanoargentate(I) complex, [Ag(CN)₂]⁻. The gangue (rock) does not dissolve, so the silver is selectively leached.

### Step 2 — Precipitation (Reduction with Zinc)

The leach solution is treated with scrap zinc (Zn powder):

2[Ag(CN)₂]⁻ + Zn  →  [Zn(CN)₄]²⁻ + 2Ag↓

Silver is displaced because Zn has a more negative E° than Ag (Zn is a stronger reducing agent than Ag). This is called the cementation step

### Step 3 — Refining

The precipitated silver is filtered off and further purified by electrolytic refining.

## 4.2 Cyanide Process for Gold

The process is essentially the same as for silver.

### Step 1 — Leaching

4Au + 8CN⁻ + O₂ + 2H₂O  →  4[Au(CN)₂]⁻ + 4OH⁻

Gold dissolves as the stable dicyanoaurate(I) complex, [Au(CN)₂]⁻.

### Step 2 — Precipitation with Zinc

2[Au(CN)₂]⁻ + Zn  →  [Zn(CN)₄]²⁻ + 2Au↓

### Alternative: Activated Charcoal

In the modern CIP (Carbon-in-Pulp) process, activated charcoal adsorbs the gold complex, which is then eluted and the gold recovered by electrolysis.

Why Cyanide? The Role of Complex Formation

Gold and silver are extremely stable metals (very positive E°) and do not dissolve in most acids or bases. The cyanide ion (CN⁻) is a strong ligand that forms exceptionally stable complexes [Au(CN)₂]⁻ and [Ag(CN)₂]⁻. The high stability of these complexes (large formation constants) shifts the equilibrium to the right, making dissolution thermodynamically favourable even though Au and Ag are noble metals. Environmental note: CN⁻ is highly toxic; modern plants use closed-loop cyanide recovery and CN⁻ is detoxified (e.g., oxidised to OCN⁻, then to CO₂+N₂).

| Comparison | Silver | Gold |
| --- | --- | --- |
| Ore | Ag₂S (argentite), native Ag | Native Au, tellurides |
| Leaching agent | NaCN/KCN + air | NaCN + air |
| Complex formed | [Ag(CN)₂]⁻ (dicyanoargentate-I) | [Au(CN)₂]⁻ (dicyanoaurate-I) |
| Precipitation agent | Zn (cementation) | Zn or activated carbon (CIP) |
| Formation constant | K ~10²¹ | K ~10³⁸ (much more stable) |

# 5. Methods of Purification of Metals

After extraction, metals often contain impurities and require refining. Three important methods are covered here.

## 5.1 Electrolytic Refining

This is the most widely used method for obtaining high-purity metals. Used for Cu, Ag, Au, Ni, Pb, and Sn.

### Principle

The impure metal is the anode, the pure metal is the cathode, and a solution of a soluble salt of the metal is the electrolyte. On passing current, the anode dissolves and pure metal deposits on the cathode.

### Process (Example: Copper)

- Anode: Impure copper (contains Zn, Fe, Ni, Au, Ag, Pt impurities)

- Cathode: Pure copper sheet

- Electrolyte: Acidified CuSO₄ solution

- Anode reaction: Cu → Cu²⁺ + 2e⁻  (and all less noble impurities: Fe, Zn, Ni dissolve too)

- Cathode reaction: Cu²⁺ + 2e⁻ → Cu  (only Cu deposits; Fe²⁺, Zn²⁺, Ni²⁺ stay in solution)

What Happens to Impurities?

Active impurities (Fe, Zn, Ni — more negative E° than Cu): Dissolve at anode but do NOT deposit at cathode (their E° is more negative than Cu²⁺/Cu). They accumulate in the electrolyte solution. Noble impurities (Au, Ag, Pt — more positive E° than Cu): Do NOT dissolve at anode. They fall below the anode as anode mud / anode slime. Recovered as valuable by-products.

## 5.2 Van Arkel-De Boer Process (Vapour Phase Refining)

Used for obtaining ultra-pure metals, especially titanium (Ti) and zirconium (Zr). Also used for V, Hf, Th, and Si.

### Principle

The crude metal is converted to a volatile compound (iodide) at low temperature, and the compound is then thermally decomposed at high temperature on a hot filament, depositing pure metal.

### Steps for Titanium

- Step 1 — Iodide formation (250°C): Ti(crude) + 2I₂ → TiI₄(g)  [volatile iodide formed]

- Step 2 — Decomposition (1400°C): TiI₄(g) → Ti(pure) + 2I₂  [on hot tungsten filament]

- Cycle: I₂ is regenerated and cycles back to react with more crude Ti. The impurities do not form volatile iodides and remain behind.

Key Features of Van Arkel-De Boer Process

- Produces metals of extremely high purity (99.99%+). - The iodide acts as a chemical shuttle — carries pure metal and leaves impurities behind. - Impurities (like oxygen, nitrogen, carbon in crude Ti) do not form volatile iodides, so they remain in the crude zone. - Also called the Iodide Process or Crystal Bar Process (the pure Ti deposits as a crystal bar on the filament). - Disadvantage: Expensive and slow; used only when very high purity is needed.

## 5.3 Zone Refining

Also called Pfann's Zone Refining (developed by William Pfann, Bell Labs, 1952). Used to purify semiconductors (Si, Ge), metals (Ga, In, Bi), and organic compounds

### Principle

Based on the difference in solubility of impurities in solid vs. liquid metal. Most impurities are more soluble in the liquid phase than in the solid phase (distribution coefficient K < 1). As the molten zone moves, impurities concentrate in the liquid and are swept to one end.

### Process

- The impure metal rod is placed horizontally in an inert atmosphere.

- A circular heater (induction heater) creates a narrow molten zone at one end.

- The heater slowly moves from one end to the other. The leading edge of the zone melts new solid (picking up impurities); the trailing edge solidifies (leaving purer metal behind).

- After many passes, impurities accumulate at one end, which is cut off.

Why Do Impurities Move to One End?

If the distribution coefficient K = Cs/Cl < 1 (concentration in solid / concentration in liquid), the impurity prefers the liquid phase. As the molten zone sweeps forward, impurities jump into the liquid zone and travel with it to the end. After multiple passes, the far end is heavily contaminated and the rest is very pure. For Si and Ge: purity levels of 1 part per billion (ppb) are achievable — essential for semiconductor manufacture.

| Method | Principle | Metals Purified | Purity Level |
| --- | --- | --- | --- |
| Electrolytic Refining | Anode dissolves; impurities either stay in solution or fall as slime | Cu, Ag, Au, Ni, Pb, Sn | 99.95–99.99% |
| Van Arkel-De Boer | Volatile iodide formed at low T; decomposes at high T on hot filament | Ti, Zr, V, Hf, Si | 99.99%+ |
| Zone Refining | Impurities more soluble in melt; swept to one end by moving molten zone | Si, Ge, Ga, In, Bi | Parts per billion |

# 6. Metals and Alloys in Ancient and Medieval India

India has one of the longest and richest traditions of metallurgy in the world. From the Indus Valley Civilisation (~3000 BCE) to the medieval period, Indian craftsmen and metallurgists made advances far ahead of contemporary civilisations in several areas.

## 6.1 Copper and Bronze Age India

| Metal / Alloy | Period | Key Points |
| --- | --- | --- |
| Copper | ~3500 BCE (IVC) | Earliest metal used; arrowheads, mirrors, vessels found at Mohenjodaro and Harappa |
| Bronze (Cu+Sn) | ~2500–1000 BCE | Used for weapons, tools, sculptures; bronze casting at high level |
| Brass (Cu+Zn) | ~200 BCE onwards | Indians may have been among earliest users of brass; zinc smelted at Zawar (Rajasthan) |

## 6.2 Iron and Steel

### Iron Smelting

India developed iron smelting independently around 1800–1200 BCE (some claims push this to ~1900 BCE in peninsular India — among the earliest in the world). Iron was used for tools, weapons, and agricultural implements.

### Wootz Steel (Crucible Steel)

India developed Wootz steel (also called Damascus steel when it reached the Middle East) around ~300 BCE–200 CE, which was far superior to any contemporary steel. It is characterised by:

- High carbon content (1.0–1.8%) — hypereutectoid steel.

- Distinctive watered / wavy pattern on the surface due to carbide banding.

- Exceptional sharpness and toughness — legendary for sword blades.

- Made by melting iron with carbon-rich materials (wood, leaves) in sealed clay crucibles.

### Iron Pillar of Delhi

Iron Pillar of Delhi — A Metallurgical Marvel

Location: Qutb complex, New Delhi. Date: ~4th–5th century CE (Gupta period, probably under Chandragupta II). Composition: ~98% pure wrought iron (low carbon, low sulphur, high phosphorus ~0.1–0.25%). Height: ~7.21 m; Weight: ~6 tonnes. Corrosion resistance: Has stood for ~1600 years with minimal rust. Modern analysis shows a thin protective layer of misawite (δ-FeOOH) and crystalline iron phosphate (FePO₄) forms naturally, sealing the surface against further oxidation. Why resistant? High phosphorus content promotes the formation of this protective layer. Also, the wrought iron was slag-hammered while hot — a purification technique that removed much oxygen.

## 6.3 Zinc Smelting — Zawar, Rajasthan

India is credited with the world's first industrial-scale zinc smelting. The Zawar mines in Rajasthan (near Udaipur) show evidence of distillation-based zinc smelting dating to ~9th century CE, reaching its peak around 14th–18th century CE.

- Zinc ore (ZnO or ZnCO₃) was reduced with charcoal in sealed clay retorts.

- Zinc vapour (bp 907°C, below the retort temperature) was collected by downward condensation — a unique technique used because zinc vapour must be rapidly cooled below its boiling point to prevent re-oxidation.

- Estimated production: up to 200 tonnes/year at peak.

- European zinc smelting only began in the 17th century, nearly 800 years later.

## 6.4 Gold and Silver

| Metal | Historical Significance |
| --- | --- |
| Gold | Used since Indus Valley; extensive goldsmithing; panning of alluvial gold in Kolar (Karnataka); used in Panchalohā (5-metal alloy) |
| Silver | Widespread use for coinage (punch-marked coins, ~600 BCE+); extracted from Ag₂S by cupellation process (lead-silver ore smelted; lead oxidised to PbO in blast of air, leaving Ag) |

## 6.5 Mercury

Mercury (Parada) was known in India by at least ~300 BCE and is described extensively in Rasashastra (the Indian science of alchemy and medicine using metals and minerals). Cinnabar (HgS) was roasted to obtain mercury vapour, which was condensed. Mercury was used in medicinal preparations, as amalgams, and in extraction of precious metals.

## 6.6 Important Alloys of Ancient/Medieval India

| Alloy | Composition | Use |
| --- | --- | --- |
| Panchaloha | Au, Ag, Cu, Zn, Fe (or Sn in different traditions) | Temple idols, ritual objects; still used today |
| Ashtadhatu | 8 metals: Au, Ag, Cu, Zn, Pb, Fe, Sn, Hg (varies by tradition) | Idols, ritual items |
| Wootz / Damascus Steel | Fe + C (1–1.8%) + trace elements | Sword blades; legendary cutting edge |
| Bell metal (Kansa) | Cu + Sn (~20–22% Sn) | Bells, vessels, utensils; higher Sn than typical bronze |
| Brass (Pittala) | Cu + Zn | Vessels, coins, ornaments |
| Bidri alloy | Zn (90–94%) + Cu (4–6%) + trace Pb, Sn | Decorative bidriware (Bidar, Karnataka); metal black after nitriding |

Rasashastra — Indian Alchemy and Metallurgy

Texts like the Rasaratnākara (attributed to Nāgārjuna, ~8th CE), Rasahṛdaya Tantra, and Rasendra Cūḍāmaṇi document detailed methods for: purifying metals (shodhana), preparing calxes (bhasma), zinc distillation, mercury amalgamation, and the preparation of alloys. The tradition represents a sophisticated empirical chemistry that predated much of European alchemical knowledge in several domains.

# Quick Revision: Key Points

| Topic | Key One-liners |
| --- | --- |
| Occurrence & E° | Very negative E° → combined state; very positive E° → native/free state |
| Ellingham diagram | Plot of ΔG° vs T for oxidation; reducing agent line below = reduction feasible |
| C vs CO | C (→CO) line has steep negative slope; wins at high T. CO is flat; effective at low–moderate T |
| C can't reduce | Al₂O₃, MgO, CaO — their lines lie far below C's line |
| Hall-Héroult | Al₂O₃ dissolved in cryolite at 960°C; C anode (consumed); Al at cathode |
| Down's process | Molten NaCl+CaCl₂; Na at cathode; Cl₂ at anode |
| Cyanide process | Ag/Au leached as [M(CN)₂]⁻; precipitated with Zn; complex stability drives dissolution |
| Electrolytic refining | Impure metal = anode; pure metal = cathode; noble impurities → anode slime; active impurities → solution |
| Van Arkel-De Boer | Crude Ti + I₂ → TiI₄(g) at 250°C; TiI₄ → Ti(pure) + I₂ at 1400°C on filament |
| Zone refining | K=Cs/Cl<1; impurities prefer melt; swept to end; ppb purity for Si/Ge |
| Iron Pillar | ~4th–5th c CE; 98% wrought iron; protected by FePO₄/δ-FeOOH layer; stands 1600 yrs |
| Zawar zinc | World's first industrial Zn smelting; ~9th–18th c CE; downward condensation technique |
| Wootz steel | ~300 BCE; high C (~1.5%); wavy pattern; crucible process; basis of Damascus steel |
| Panchaloha | 5-metal alloy (Au, Ag, Cu, Zn, Fe); used for temple idols |

End of Unit I — General Principles of Metallurgy